







JOURNEY’S END 







Hardwood Flooring Specialist



93 Grand Drive, Raynes Park, SW20 9DW Tel: 07831 258344
	Kredenza

	Southolm Street

	London

	SW11

	

	Ref East Weald


Dear Deyan

Further to our site visit at the above address, it was noted that the existing parquet is traditional oak, quarter sawn and laid in a herringbone design, with an inlaid border.

The main problem with the existing floor is that the parquet has ‘cupped’ (bowing upwards at both ends) due to floor being a square edged product, it is not possible to re-pin the floor to its original form.
Than main reason for this is, if you were to use a re-pinning process, you would be under mining the existing adhesion and if we were to re-pin & try to reverse the situation, the battens would spilt due to the pressure being re-applied and parquet should not be put under pressure under any circumstances.

The existing adhesion in this case is a PVA type adhesive, with the parquet being glued and pinned to existing floorboards.
If any contractor were to proceed with a refurbishment process the problem would re-occur as soon as any heating was introduce into the building as the flooring has been exposed to an unacceptable ingress of water and a prolonged period of dereliction.
Due to the fact that this is a straight grained 3/8” thickness product, it is not deigned to recover from this type of exposure.
The original panel pins that are were used to secure the battens have deteriorated due to their age and material composition and therefore cannot be punched below the surface to enable any type of cleaning or sanding process

We would therefore conclude that the existing floor could not be successfully repaired and any such attempt would result in failure.

The only alternative therefore is to replace the floor with a similar product cut from a re-claimed source.
Yours Sincerely

Frank O’Donoghue

fodonoghue@btinternet.com


