Hard Flooring Prep Info

Plywood

Marine plywood is manufactured from durable face and core veneers, with few defects so it performs longer in both humid and wet conditions and resists delaminating and fungal attack. Its construction is such that it can be used in environments where it is exposed to moisture for long periods.

It uses an exterior Water and Boil Proof (WBP) glue similar to most exterior plywoods. Marine plywood can be graded as being compliant with BS 1088, which is a British Standard for marine plywood. There are few international standards for grading marine plywood and most of the standards are voluntary.

Screeds
Stopgap 300 Powder Mixed with Water (coverage per 25kg bag = 5m2 @ 3mm thick)
A rapid hardening, water mix smoothing underlayment. It is designed for use on both absorbent and non-absorbent interior sub floors, in areas that are subjected to heavy-duty trafficking.

The underlayment has excellent smoothing properties making it suitable for application by mechanical pump or by traditional mixing methods.

Stopgap 700 Powder Mixed with Water (coverage per 20kg bag = 4.8m2 @ 3mm thick)
Fast drying, flexible, fibre-reinforced self-smoothing underlayment, designed specifically for use over plywood. Based on the latest advances in cement and polymer technology, enabling fast track application prior to the installation of new floor coverings.

Can be applied between 2mm and 10mm to a wide range of sub floor types. Due to fast drying technology it is ready to receive most floor coverings in as little as 3 hours.

