| Product Name | Milano (27) |
| --- | --- |
| Construction | Flat Woven |
| Product Description | Textured Tweed Loop |
| Suitability: EN 1307 Class 23/32 | Heavy Domestic / Medium Contract |
| Rows (Picks) | 17.00 / 10cm |
| Reed | 51.80 / 10 cm |
| Tuft Density | 88,060/m2 |
| Pile Height above Backing | 9mm |
| Total Pile Weight | 1614g/m2 |
| Total Carpet Weight | 3230g/m2 |
| Pile Fibre Content | 100% Wool (Moth Proofed) |
| Backing Materials | Warp: Wool & Cotton Weft: Wool & Jute Secondary Backing: Jute |
| Widths Available | 5m |
| Colour Fastness: - Light - Shampoo - Wet Rub | 5 4 5 |
| Static Loading | Thickness Recovery 84% |
| Abrasion Resistance | In excess of 25,000 rubs |
| Tog Rating | 1.20 |
| CE Mark (reaction to fire): EN 1350 | EN 14041 : 2004 Class: Cfl-s1 Slip: NPC |
| Flammability Ratings: Hot Metal Nut Test | Low radius effects of ignition |
| Stock Range Colour References; | 441 – Marrone 442 – Tartufo 443 – Sabbia 444 – Carbone 445 – Grigio 446 - Argento |
| All the above specifications above are subject to normal manufacturing tolerance variations Batch to Batch Colour Matching Whilst every effort is made to insure that the colours are matched as accurately as possible from one batch to another an exact match, particularly with natural undyed wools, cannot be guaranteed. If you wish to have an exact colour please request a dye batch cutting from your authorised dealers before ordering stock. Shading Carpets may develop light and dark shaded areas, particularly in heavy traffic areas, this is called shading and is caused by pile pressure. This is not considered to be a manufacturing defect and can occur on most textiles. Installation Carpets should always be installed by a fully trained and experience installer and full in accordance with our installation guidelines. Care & Maintenance If installed and maintained correctly your carpet should give you years of good service. We recommend that spillages are spot cleaned immediately and that you use a professional carpet cleaning contractor to look after your carpets. |  |